STAR ELASTO-BOND 3405

(Crack and Joint Sealant)

# STAR ELASTO-BOND 3405 Crack and Joint Sealant;

- Low Penetration

- Self-Leveling

- Rapid Melting

- Flexible to -20(F

- Excellent Adhesion

- Sets-Up Quickly

- Resists Tracking

## Recommended Uses:

STAR Elasto-Bond 3405 is recommended for sealing cracks and joints in Portland cement, asphaltic pavements, and parking lots. It is designed to seal expansion and contraction joints, longitudinal and transverse cracks, joints between concrete and asphaltic shoulders, and random cracks.

Typical Properties:

Recommended Application Temp . . . . . . . . . . . . . . . . . . . . 370 - 390ºF

Maximum Heating Temp . . . . . . . . . . . . . . . . . . . . . . . . . . . . .  . . 410ºF

Maximum Heating Time . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . 12 Hrs.

Penetration (150 gr./5 sec) . . . . . . . . . . . . . . . . . . . . . . . . . . . . 90 Max.

Resiliency . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . 60% Min.

Flow at 140ºF . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . . 3 mm Max.

Bond, -20ºF/50% Ext . . . . . . . . . . . . . . . . . . . . . . . . . . Passes 3 Cycles

0ºF/100% Ext . . . . . . . . . . . . . . . . . . . . . . . . .. . . . . . . Passes 3 Cycles

Specific Gravity . . . . . . . . . . . . . . . . . . . . . . .  . . . . . . . . . . . . . . . . 1.14

Asphalt Compatibility . . . . . . . . . . . . . . . . . . .. . . . . . . . . . . Compatible

### Coverage

Width         	Depth        	Pounds/100

Linear Feet

3/8”           	3/8”             	6.9

3/8”           	1/2”             	9.3

1/2”           	1/2”           	12.3

1/2”             	1”           	24.7

3/4”            	1/2”          	18.5

3/4”            	3/4”          	27.8

#### Specifications:

ASTM-D3405

ASTM-D6690 Type II & III

AASHTO-M301

Exceeds

ASTM-D1190

ASTM-D6690 Type I

AASHTO-M173

Fed. Spec. SS-S-1401

Packaging:

STAR Elasto-Bond 3405 is packaged in 2-25 lb. poly-bags in a 50-lb. High strength corrugated box.   Each Pallet contains 48 boxes or approximately 2400 pounds of STAR Elasto-Bond 3405.

Surface Preparation:

Proper surface preparation facilitates adequate adhesion and consequently the maximum life of the sealant. In order for proper adhesion, the crack/joint must be free of moisture, dust, loose aggregate, and other contaminates. The substrate and air temperatures must be 40ºF or above. Sawing, routing, and/or sandblasting are the preferred methods of preparation. Use oil-free compressed air and heat to clean and dry the joint immediately prior to sealing. Cracks/joints should be sized so that the maximum extension and compression do not exceed 50% of the width. Best results are obtained when the cracks/joints are opened at least 1/2 inch wide.

Melting and Application:

The melting kettle should be a conventional oil jacketed unit equipped with an agitator and temperature control devices for both the material and heat transfer oil. Carefully insert small quantities of STAR Elasto-Bond 3405 and the plastic bag into the melting equipment while the agitator is turned off. Load material slowly to avoid splash back. After the initial load has reached the recommended pouring temperature, fresh material may be added to the melter as sealant is used. Melt only the material that will be used during that day. Purge material remaining in the kettle lines at the end of each sealing operation. The material may be safely reheated and can be applied using a pressure feed wand system or a pour pot.

Note:

The temperature of the heat transfer oil should not exceed 525ºF. Do not heat STAR Elasto-Bond 3405  above the maximum heating temperature and do not maintain it at that temperature for prolonged periods of time. This could cause the material to gel in the equipment or fail in the cracks/joints. A significant viscosity increase accompanied by stringiness signals the approach of gelation. If this occurs, immediately remove the material from the melter and dispose of it.

# Text boxes

PRODUCT BULLETIN

1150 Milepost Drive

Columbus, OH  43228

(614)870-0744

Fax: (614)870-0598

800-759-1912

www.starseal.com

1400 Walcutt Road

Columbus, OH  43228

(614)870-0744

Fax: (614)870-0598

800-759-1912

www.starseal.com